## Slide 1: RUNGTA COLLEGE OF DENTAL SCIENCES AND RESEARCH
DENTAL CEMENTS
DEPARTMENT OF CONSERVATIVE DENTISTRY AND ENDODONTICS

## Slide 2: Specific learning objectives at the end of this presentation the learner is expected to know ;
Core areas* | Domain ** | Category #
Introduction | Cognitive | Must know
classification | Cognitive | Must know
Compositions | Cognitive | Must know

## Slide 3: Contents
Introduction
Key terms
Agents for pulp protection
Ideal requirements
Classifications
Properties
composition

## Slide 4
Glass Ionomer Cements:
ADA specification No is
Adhesive tooth coloured restorative material
Invented by Wilson & Kent in 1972.
Originally used for restorations of eroded areas.
Subsequently modified to allow its use in other areas.
Has combined properties of silicate cements & polycarboxylate cements.
As a restorative material requires minimal cavity preparation.

## Slide 5
This cement is also known as….
Poly (alkenoate) cement
GIC
ASPA (Alumino silicate ployacrylic acid)
Applications:-
1. Anterior esthetic restorative material
2. eroded areas & class V restorations
3. As a luting agent
4. as liners and bases
5.for core build up
6. as pit and fissure sealant to some extent

## Slide 6
Classification:-
Type I …..For luting
Type II ….For restorations
Type III…. Liners and bases
Commercial names:-
Aqua chem …. Type I
FUGI I ….. Type I
CHEM Fil ….. Type II
Logo Fil….. Type II
Ketac bond …. Type III
Vitra bond ….. Light cure GIC

## Slide 7
Mode of supply:-
Powder/ Liquid in bottles
Pre-proportioned powder/Liquid
Light cure system.

## Slide 8
Composition:-
Powder:
Silica ….. 41.9
Alumina…. 28.6
Aluminum fluoride …. 1.6
Calcium fluoride….. 15.7
Sodium fluoride….. 9.3
Aluminum phosphate…. 3.8

## Slide 9
Liquid:-
Polyacrylic acid- In the form of copolymer with itaconic, maleic
or tricarboxylic acid to…
1. To increase the reactivity of the liquid
2.Decrease viscosity
3.reduce tendency for gelation
Tartaric acid
1. Improves the handling characteristics
2. Increases working time
3. Shortens setting time.
Water
Most important constituent of the cement liquid.
It is reaction medium and it hydrates the reaction products.

## Slide 10
Water settable cements:-
The polyacrylic acid copolymer may be freeze dried and mixed with glass ionomer powder
The Liquid is water or water with tartaric acid.
Manufacturing of the powder
The raw material components are fused at temp 1100-1500°C
The glass is ground to particle size- 20 to 50 u
Setting reaction:-
Powder &Liquid mixed together
Calcium polysalts forms first and later aluminum polysalts
The salts hydrate to form a gel matrix
The unreacted glass particles are sheathed by silica gel.

## Slide 11
Structure of set cement
Consists of agglomerates of unreacted powder particles surrounded by silica gel and embeded in an amorphous matrix of calcium and aluminum polysalts.
Setting time
Type I…. 4 to 5 minutes
Type II…. 7 minutes.

## Slide 12
Properties:-
Mechanical
Compressive strength- 150 Mpa (less than silicate cement)
Tensile strength- 6.6 Mpa (higher than silicate)
Hardness- 48 KHN
Fracture toughness- much inferior to composite
Solubility and Disintegration
Initial solubility is high due to leaching of intermediate products
or those not involved in matrix formation.
Solubility is…0.4%
Mechanism of Adhesion
Chemical bonding is due the reaction between the Carboxyl groups of the polyacids and the calcium in the apetite of the enamel and dentin.

## Slide 13
Esthetics
They are inferior to silicates and composites in this respect.
They lack translucency
Have a rough surface texture.
Biocompatability
Relatively biocompatible.
Mild pulpal response.
Anticariogenic properties
Physicochemical mechanism
Biologic mechanism

## Slide 14
Manipulation:-
For a successful restoration of glass ionomer cement the rules to be followed are,
Conditioning of the tooth surface.
Proper manipulation.
Protection of cement during setting.
Finishing.

## Slide 15
Procedure
The powder and liquid is dispensed on to a paper pad
The powder and liquid ratio is 3:1 by weight
The powder is divided in to two equal increments
The first increment is incorporated in to the liquid rapidly
with the stiff bladed agate spatula by folding method,
to produce homogenous consistency with glossy appearance.
The mixing time is 45 seconds.
The mixed cement should be immediately packed in to the cavity.

## Slide 16: Restoration of GIC and removal of excess
As a restorative material requires minimal cavity preparation.
The restorative cement mixture is applied by a plastic instrument.
Tooth cavities should be slightly overfilled with cement.
The surface should be covered with a plastic matrix to protect the setting from loosing or gaining water during the initial set.
The matrix should be kept in place for 5 minutes.
After removal of the matrix, the surface must immediately be protected while the excess material is trimmed from the margins.

## Slide 17
THANK YOU

## Slide 18
Zinc silicophosphate cement
Has resulted from combination of zinc phosphate cement & silicate powders
A.D.A. specification -21
Type 1 cementing medium
Type 2-temporary posterior filling material
Type 3- both uses
Anticariogenic due to Fl release
High compressive strength- 165 Mpa.
Semitransluscency
Uses-luting agent
intermediate restorations
As a die material.

## Slide 19
Resin cements
They are filled & unfilled resins
Supply – powder & liquid system
- two paste system
Setting 4-10 min
reaction – chemical [ peroxide –amine induction ]
-light activation
Enamel bonding by acid etch
Dentin bonding by dentin bonding agents
Irritant to pulp
Insoluble in oral fluids
Use cementation of porcelain veneers ,crowns& bridges

## Slide 20
Copper cement
Copper oxide ,[cuprous –red, cupric –black]
Zinc oxide
they are bacteriostatic & bactericidal
irritant to pulp-Ph 5.3
USES:
Temporary fillings in children
Inermediate restorations

## Slide 21: Metal modified Glass ionomer cement
Introduced in an attempt to improve ,
Strength.
Fracture toughness.
Resistance to wear.
Two methods are employed,
Silver alloy admix.
Cermet.

## Slide 22: Properties
Mechanical properties
Compressive strength- 150 Mpa
Anti cariogenic property
Esthetics.
Clinical considerations
Class I cavities in young patient.
Core build up material.

## Slide 23: Resin modified Glass ionomer cement
Convential GICs set by acid base reaction
Two inherent drawbacks of GIC are….
1.Moisture sensitivity
2.Low early strength
Addition of polymerizable functional group-HEMA
Set partly by acid base reaction and partly by photochemical polymerization

## Slide 24
Composition
Powder Liquid
Ion leachable glass water
Initiator for light curing Polyacrylic acid
Iniator for chemical curing polyacrylic acid with some
Carboxylic group modified with HEMA

## Slide 25
Physical properties
Strength
Adhesion to tooth
Adhesion to restorative material
Marginal adaptation
Water sensitivity
Clinical considerations:-
1. Liner
2. Fissure sealant
3. Core built up
4. Ortho brackets
5. Repair of restorations

## Slide 26: Take home message
It is type of direct restorative material which may be defined as the substance that hardens to act as base, liner, filling material, or adhesive to bind devices and prostheses to tooth structure or to each other. Dental cements used as restorative materials have low strengths compared with those of resin-based composites and amalgam.

## Slide 27: Questions
Define dental cements
What are different classification of dental cements ?
Give composition of different cements ?

## Slide 28: Suggested reading
Basic dental materials by manappallil
Philip’s science of dental sciences

## Slide 29
Thank you